（V2XY_V2XH_V2XC_V2XK_V31N_V3L6）顾客特殊要求
	更新项目序号
	更新项目名称
	更新时间
	客户协议编号

	CAM部分
	4.文件要求
	20230606
	SE0003/FI0002/NO0003/HK0033/NL0006/663389客户特殊要求.docx许宋如2023-04-24顾客质量要求评审表

	共用部分
	7.阻流铜要求
	
	

	标题位置
	新增代码V3L6
	20221109
	663389663389(V3L6)要求.docx许宋如2022-11-04顾客质量要求评审表

	预审部分
	3.EQ要求
	20220729
	SE0003_FI0002_NO0003_HK0033_NL0006EQ完整性.zip许宋如2022-07-25顾客质量要求评审表

	CAM3
	ERP备注
	20170328
	V2xy20170349

	预审部分：3
	V2XY增加要求
	20160726
	V2XY20160740

	预审部分:1;2
	材料;顾客制板说明
	2016.04.01
	销售

	
	
	
	


备注：更新的内容以蓝色字体显示。
共用部分：
1.优先等级：制板说明中的要求>该部分顾客要求
2.标记:按顾客制板说明中的要求加标记，无标记要求时，与顾客确认

3.阻焊桥:顾客文件中有阻焊桥，则必须保证有阻焊桥，无法做到时，则与顾客确认

4.钻孔:若需要二钻孔，则需要与顾客确认（顾客要求一次钻孔）

5.工艺边:若有工艺板，则工艺边需要倒0.5-1.0mm的圆角，顾客有设计好的除外。

6.蓝胶：

    无要求时，蓝胶厚度0.3-1.0mm（技术中心评审结果：印两次蓝胶可满足）

     蓝胶型号只能用：SD2955-SW
7.阻流铜要求

1).不允许在板内添加阻流铜
2)如果在工艺边上添加阻流铜，阻流铜必须与光学点距离2.5mm以上
3)阻流铜的形状不允许与mark点形状相同

预审部分： 
         1.材料: 如果客户要求板材符合IPC4101C-124/126优先建议使用 IT-180A.

          2.顾客制板说明:客户说明文件中要求要符合“2014020 supplier Manual”,预审可以不用理会，因为该要求已经转入该部分客户要求中
[image: image1.jpg]When preparing production files of part number you must also follow instructions in our latest
version of document 2014020 Supplier Manual®s

e





=============================
          3.V2XY顾客增加如下要求（需要预审指示给CAM）：
            客户有下图的要求,需要在工艺边上铺满网格. 类似给出的实物板效果如下：

        [image: image2.png]PEELABLE MASK
V- cUT FILE
STAMP HOLE FILE

ER TR DOZRE BEERREL D LHEH I
R

Required balance of copper on full frame acording picture -
p——————




 3.EQ要求：在EQ沟通过程中需保持所有的EQ内容在一个Excel文档里，如下图. 添加EQ状态栏，所有的EQ在一页里 
[image: image3.png]No Problem Description Kinwong Suggestion image_[ustomer Confirmatior] | EQ Status.
T [We couldnt do “FTH_through” for s board dus fo e _|Changing this holes(6 X & 0mm) to NPTH_through. WG1 (oK o5
metal substate s Aluminu. Aluminum wil be dissolved by [Please confirm?
electropiatng soluton, (4.0mm holes. need il L o
| Auminu )
T3 [The holes(94 0mm) s tangent wi e L2 layer copper | Trimming the copper to keep 0 45mm Clearance away fomine | LIG1Z |OK Cosen
and the min space is too smal, & wil cause burrs for he [noe to meet the Hi -Pot test and burrs
fnshed board and which s unavoidable and cant meet
the Hi-Pot test Please confirm?
T4 [This s single-sided doubl layers board, £ requires _|A. Changing fo ENG surface treatment we wil update he RFQ. | 1112 | ADWINTREENIGAVE BR[O CLOSED
HASLLead free surface treatment and designs no [affect o the via opening?|
|solder mask opening for the PTHs During HASLALF (8. we propose to add solder mask opening (0.1mm smaler per
process, the high temperature may lead fo the solder [side than the vias) to the vias designed covered with sokder
mask nk exuded. mask nk o do. I the PTH poston could not keep sokder mask.
oridges, we wil doing whole solder mask opening.
Please make a choice.
Changing the surface treatment 1o ENG,we wilbe [ Pleass kindly know that
folow the orignalgerber todo dont need add the [ Thank you
14- |soider mask opening for PTH'.
E
15 [The pads are only 020 0.55mmor 021 *0.55mm, & _|A. Following geber but pis accept nonwettng LG |8 CLosen

won't get wetiing during HASL process(require a
minimum of width 0.25mm)

Changing the surface treatment to ENIG we wil update he.
Rra.
Please choose AorB 7





CAM部分： 
1打叉要求:不允许打叉
2.补线要求:不允许补线
3.ERP备注:

      阻焊工序备注:阻焊不允许套印

      终检工序备注: 阻焊不允许套印,沉金板不允许补镍.

 4.文件要求：GERBER资料，叠层资料，贴片文件，拼板尺寸图需要提供给客户。
